[image: image1.jpg]



the hashemite kingdom of jordan
the jordanian electric power company limited

Specification JEP 44/2026


tender document for

aluminium meter seals & stainless steel wires 
	Tenderer's Name:
	____________________

	Address:
	____________________

	Closing Date:
	____________________

	Closing Time:
	____________________


May   2026
THE JORDANIAN ELECTRIC POWER COMPANY LIMITED

AMMAN   –  JORDAN

	Telephone 962 6 5503600

P.O. BOX 618

ZIP CODE 11118
	____________
	CABLE: ELECTRICO

FAX 962 6 5503618

EMAIL: specs@jepco.com.jo


SPECIFICaTION  JEp 44/2026 
aluminium meter seals & Stainless steel wires
1. GENERAL
Item (1): Stainless steel wires

· The stainless steel wire grade AISI 316 shall be made according to UNI 6900-71 standard.

· The minimum tensile strength value shall not be less than 550N.

· The external diameter of the stainless wire shall be 1.1mm.

· The stainless steel wire rope has to be composed of three triangular strands each made of three conductors (3x3), lay R.R.L.

· The stainless steel wire shall be on roll of 1,000 meters (TOLERANCE (3%).

Item (2): aluminium meter seals

The required seals shall be manufactured according to the following specifications:

· The seals shall be shining.

· The length of Aluminum seal shall be 16 mm.

· The Aluminum seal shall have through hole of 2.3 mm diameter.

· The Aluminum seal shall have outer diameter of not less than 5 mm.

· The tensile strength of the Aluminum seals shall be 120-130N/mm2.

· The Aluminum composition shall be not less than 99.5%

· The compositions of the impurities in the aluminum seals shall not exceed those listed in the following table, with a total not exceeding 0.5%

	Impurity
	Si
	Fe
	Cu
	Mn
	Mg
	Zn
	Ti
	Other
	Total

	Composition%
	(0.25
	(0.40
	(0.05
	(0.05
	(0.05
	(0.07
	(0.05
	(0.03
	(0.50


· The meter seals shall be supplied in plastic bags, each bag contains 500 meter seals.

2. scope of work
The works shall comprise the design, manufacture, testing and delivery to the Port of Aqaba, The Hashemite Kingdom of Jordan of the equipment listed in this Specification, equipment in accordance with the Conditions of Contract at prices stated in the Schedule of this Specification, together with the provision of certain specified spares.

	Item No.
	Description
	Quantity

	1.
	Stainless steel wire
	200,000 Meters

	2.
	Aluminum Meter Seals
	1,500,000  each


SCHEDULE (A)

Summary Schedule
Technical and Commercial Data

Note: The following schedule represents the most essential data based on which the evaluation process shall be performed.

	Item
	Description
	Quantity
	Manufacturer / Origin
	Unit CFR to Aqaba Port Price/ Currency
	Total CFR to Aqaba Port Price/ Currency
	Delivery*
(Weeks)

	1.
	Stainless Steel Wires
	200,000

 Meter
	
	
	
	

	2.A
	Aluminum Meter Seals
	3,000 plastic bags 
(Each contains 500 Aluminium seals)
1,500,000 each
	
	
	
	

	


schedule (B)

 technical DATA 
(To be completed by the Tenderer)

Item (1): Stainless Steel Wire

	Item
	Description
	Stainless Steel Wire

	1.
	Tensile Stength of the stainless steel wire
	N
	
……………

	2.
	Outside diameter of the stainless steel wire
	mm
	
……………

	3.
	Does the stainless steel wire composed of three triangular strands each made of three conductors (3x3)?
	Y/N
	……………

	4.
	Does the stainless steel R.R.L. laid? 
	Y/N
	……………

	5.
	What is the grade of the stainless steel wire?
	
	……………

	6.
	How many meters each roll contains?
	
	……………


Item (2): Aluminium Meter Seals
	Item
	Description
	Aluminum  Seals

	1.
	Length of the Aluminum  seal
	mm
	……………

	2.
	Hole diameter of the Aluminum  seal
	mm
	……………

	3.
	Outside diameter of the Aluminum  seal
	mm
	
……………

	4.
	Tensile Stength of the Aluminum  seal
	N/mm2
	
……………

	5.
	Chemical Composition of the Aluminum  seal:

Al:
Si:
Fe:

Cu:

Mn:

Mg:

Zn:
Ti:

Other:

Total:
	%

%
%

%

%

%

%

%

%

%
	……………

……………

……………

……………

……………

……………

……………

……………

……………
……………

	6.
	No. of Aluminum  seals in each Plastic Bag
	
	……………


PAGE  
3
SPECIFICATION JEP 44/2026

